PASSPORT No 1604

JSC “Naftan”,  Novopolotsk

Motor gasoline

Specification 400091131.006-2009

Grade: AI-92-K3

Date of production: 02.08.2017

Tank: № 042                                                              Net weight: 2275 tonns

Lot number: 1604                                                        Registration number of sample: 35323

| № | Parameters | Requirements according to TRLA | Factual value | Testing method |
| --- | --- | --- | --- | --- |
| 1 | 2 | 3 | 4 | 5 |
| 1 | RON, min | 92,0 | 92,4 | STB ISO 5164-2008 |
| 2 | MON, min | 83,0 | 85,1 | GOST 511-82 |
| 3 | Density at 15 ºC, kg/m³ | 720,0-775,0 | 751,3 | STB ISO 12185-2007 |
| 4 | Fractional distillation: limits of distillation, ºC, max: 10% of gasoline; 50% of gasoline; 90% of gasoline final boiling point; volume fraction of residue in a flask, %, max volume fraction of residue and losses, %, max | 75,0 120,0 190,0 215,0 1,5 4,0 | 55,4 105,7 166,0 198,2 1,0 3,0 | STB ISO 3405-2003 |
| 5 | Vapour pressure, kPa, (summer period) | 35 - 80 | 46,9 | STB 1425-2003 |
| 6 | Lead content, mg/dm3, max | 5,0 | Abs | STB EN 237-2005 |
| 7 | Acidity, mg KOH/100 sm3, max | 3 | 0,06 | GOST 5985-79 with addition in p.4.3 of specification 400091131.006-2009 |
| 8 | Mass fraction of sour sulfur , %, max | 0,001 | 0,0001 | GOST 17323-71 |
| 9 | Oxidation stability, minutes, min | 600 | 600 | STB ISO 7536-2005 |
| 10 | Concentration of soluble gum, mg/100 sm3, max | 5 | 3 | GOST 1567-97 |
| 11 | Sulfur mass fraction, mg/kg, max | 150 | less 3,0 | STB ISO 20846-2005 |
| 1 | 2 | 3 | 4 | 5 |
| 12 | Copper strip corrosion (3 h at 50 º C), class | Class 1 | Class 1 | STB 1816-2007 |
| 13 | Water-soluble acidity and alkali | Abs | Abs | GOST 6307-75 |
| 14 | Contamination and water | Abs | Abs | p.4.4 specification 400091131.006-2009 |
| 15 | Colour | Colourless and maize yellow | Correspon-ding | p.4.4 specification 400091131.006-2009 |
| 16 | Benzene content, %, max | 1,00 | 0,07 | STB ISO 22854-2011 |
| 17 | Volume fraction of hydrocarbons, %, max: olefins aromatics | 18,0 42,0 | 0,3 39,6 | STB ISO 22854-2011 |
| 18 | Oxygen mass fraction, %, max * | 2,7 | 0,00 | STB EN 13132-2006 |
| 19 | Oxygenates content, %, max*: methanol ethanol isopropyl alcohol isobutyl alcohol tert-butyl alcohol ethers (5 and more C atoms) other oxygenates | Abs 5,00 10,00 10,00 7,00 15,00 10,00 | Abs 0,00 0,00 0,00 0,00 0,00 0,00 | STB EN 13132-2006 |
| 20 | Iron concentration, mg/dm3 ** | Abs | Abs | GOST R 52530-2006 |
| 21 | Manganese concentration, mg/dm3 *** | Abs | Abs | GOST R 51925-2002 |
| 22 | Volume fraction of N-methylaniline, % **** | Abs | Abs | GOST R 54323-2011 |

Conclusion: product corresponds to specification 400091131.006-2009.

* Characteristic doesn’t identify because oxygenates don’t use as a components of motor gasoline;

**     Accept an absence of Iron as concentration of iron less than 10 mg/dm3;

***   Accept an absence of Manganese as concentration of manganese less than 0,25 mg/dm3;

****Accept an absence of monomethylaniline as concentration of monomethylaniline less than 0,1 % vol.

Warranty period – 1 year from a date of production.