Passport № 2520

JSC “NAFTAN”  Novopolotsk

BASE  OIL  SN

Under contract

Type SN 1200

Date of production: 29.08.2017

Tank: P190                                                               Net weight: 735 tonns

Lot number: 2520                                                    Registration number of sample:  32191

| No. | Description | Requirements according to TRLA | Factually | Test methods |
| --- | --- | --- | --- | --- |
| 1 | Kinematic viscosity at 100 °C, mm2/s | 19,0-22,0 | 19,47 | STB 1798-2007 |
| 2 | Viscosity index, min | 90 | 94 | STB 1797-2007 |
| 3 | Color, CNT units, max | 6,0 | 4,5 | STB 1796-2007 |
| 4 | Solidification temperature, °C, max | -12 | -15 | STB 1557-2015 |
| 5 | Coking power, %, max | 0,5 | 0,28 | STB ISO 10370-2003 |
| 6 | Mechanical impurities, % mass., max | 0,005 | Abs. | GOST 6370-83 |
| 7 | Water content, % mass., max | 0,03 | traces | GOST 2477-2014 |
| 8 | Density at 20 °C, kg/m | - | 891,2 | STB 1468-2014 |
| 9 | Acid number, mg KOH per 1 g of oil, max | 0,08 | 0,017 | STB 1411-2003 |
| 10 | Ash content, %, max | 0,005 | 0,0048 | GOST 1461-75 |
| 11 | Sulphur content, % mass., max | 1,2 | 1,04 | STB 1420-2003 |
| 12 | Fenol content, % mass., max | 0,002 | Abs. | GOST 1057-2014 |
| 13 | Open-cup flash temperature, °C, min | 260 | 272 | STB 1651-2006 |
| 14 | Appearance at 20 °C | Clean and transparent | Corresponding | visual |

Conclusion: The product complies with contract requirements